Tender specification formparts

Formed glassfibre reinforced concrete panels for facade cladding

Status: April 2024

General

Information in the text of the invitation for tender must be reviewed and, if necessary, supplemented for the object.

Further liability by Rieder Facades GmbH is excluded. This also applies to printing and writing mistakes and to any subsequent changes. The respective national laws, standards and preliminary remarks for advanced rear-ventilated façades amended from time to time shall apply.

Loading, storage and handling provisions of the manufacturer must be observed.

General construction technique permit

Glassfibre reinforced concrete panels "fibreC" to cover exterior walls are certified with a general construction technique permit (allgemeine Bauartgenehmigung) “Z-31.4-166".

Certificate of conformance Austria

Austrian Certificate of Conformance No.: Z-6.1.2-04-4772

fibreC formparts 										__________________ rm

Technical material description

- fibreC glassfibre reinforced concrete panels produced of mineral raw materials

- Production method by extrusion

- Reinforcement by alkaline-resistant glass fibres in the matrix (CEM-Fil, approval Z-3.72-1731), 2-layer textile glass fabric (each longitudinally and cross-wise) and short fibres

- Continuous colouration of the entire panel. Liquid dyes for colouration of the cement-bound building materials correspond to DIN EN 12878. The pigments used in the liquid dyes are light-, UV- and weather-resilient and not solvable in water, alkalines or diluted acids.

- Building material class A1 not flammable pursuant to DIN 4102 | EN 13501

- Manufacturer certification: ISO 14001:2009 and ISO 9001:2008

- Crystalline silica < 0% - not detectable

- Surface protection: The surface is applied with a transparent hydrophobic coating by default.

Sizes

- Standard panel dimensions 2,500 x 1,310 mm, 3,100 x 1,310 mm, 3,600 x 1,310 mm special sizes on request

- Dimension deviation length (3.6 m)	± 3 mm	EN 12467

- Dimension deviation width (1.2 m)	± 2 mm	EN 12467

- Diagonal difference up to 1.5 m | above 1.5 m ± 3.5 mm | ± 4 mm DIN 18202

- Diagonal difference as of 2.5 m | above 3.6 m ± 5 mm | ± 6 mm DIN 18202

- Thickness 13 mm

- Thickness tolerance ± 10 % EN 12467

- Edge straightness (level 1)	± 0.1 %	EN 12467

- Rectangularity (level 1)	± 2 mm/m	EN 12467

Physical properties

- Tolerances of plan system up to 0.6 | up to 1.2 | up to 3.6 m  ± 2 mm | ± 4 mm | ± 8 mm DIN 18202

- Swelling size 0.384 mm/m

- Shrinkage size 0.737 mm/m

- Raw density (13 mm) 2.0 - 2.42 kg/dm³ EN 12467

- Bending tensile resilience > 18 N/mm² (MOR*) EN 12467, class 4

- E-modus for deformation calculation approx. 10,000 N/mm²

- E-modus for compression calculation approx. 30,000 N/mm²

- Dead weight / area weight (13 mm) 26 - 31.5 kg/m² depending on shade

- Heat expansion coefficient 10*10^(-6) 1/°k DIN 51045

- Building material class (panel | system) A1-not flammable | A2-s1,d0 - not flammable DIN 4102 | EN 13501-1

- Temperature stability depending on core moisture up to 350°

- Specific heat capacity approx. 1,000 Joule / (kg*K)

- Heat conductivity lambda: approx. 2.0 W / (m*K)

- Moisture expansion ± 0.05 % EN 12467

Weather resilience

- Water impermeability passed EN 12467

- Heat-rain alternating test passed EN 12467

- Frost resistance passed EN 12467

- Frost-thaw alternating test	passed EN 12467

- UV-light resilience DIN 12878

- Wet storage resilience passed EN 12467

- Hot-water resilience passed EN 12467

** MOR: Modus of Rupture; design values deviate from MOR according to national provisions. The national approvals and provisions on calculation of the rated resistance shall apply

Packed weather-tightly on pallets. Loading, storage and handling provisions of the manufacturer must be observed.

Ventilated façade covers on existing substructure according to technical provisions and applicable standards.

Supplier of formparts:	Rieder Facades GmbH

Gemmerstraße 21, 5751 Maishofen, Österreich

T +43 6542 690 844, office@rieder.cc, www.rieder.cc

COLOURS

Colour collection greyscale:

polar white 				_____________ rm

off-white 				_____________ rm

ivory 				_____________ rm

silvergrey 				_____________ rm

chrome 				_____________ rm

anthracite 				_____________ rm

liquid black 				_____________ rm

Colour collection bricky:

coralline				_____________ rm

terracotta 				_____________ rm

oxide red				_____________ rm

burgundy				_____________ rm

merlot				_____________ rm

Colour collection timber:

larch				_____________ rm

oak					_____________ rm

walnut				_____________ rm

ebony				_____________ rm

terra				_____________ rm

Colour collection pietra:

cotton				_____________ rm

vanilla				_____________ rm

sahara				_____________ rm

sandstone				_____________ rm

almond				_____________ rm

Other Colours:

green				_____________ rm

SURFACE formparts sharp-edged

ferro: sandblasted surface

ferro light: slightly sandblasted surface

matt: smooth, brushed surface

SURFACE formparts round-edged

ferro: sandblasted surface

ferro light: slightly sandblasted surface (on request)

Special Textures Formparts sharp-edged

terrazzo black ferro plus		_____________ rm

vintage matt				_____________ rm

groove ferro soft			_____________ rm

groove ferro light			_____________ rm

groove ferro				_____________ rm

twine ferro soft			_____________ rm

twine ferro light			_____________ rm

twine ferro				_____________ rm

salt’n’pepper ferro plus		_____________ rm

salt’n’pepper ferro			_____________ rm

luce silver ferro			_____________ rm

lumber ferro				_____________ rm

slate ferro soft			_____________ rm

special textures Formparts round-edged

salt’n’pepper ferro plus		_____________ rm

salt’n’pepper ferro			_____________ rm

luce silver ferro			_____________ rm

FORMPARTS

U-shape: 							_______________pcs.

Edge			rounded 	sharp

Length in mm		_____________________________

Back in mm 		_____________________________

Leg 1 in mm		_____________________________

Leg 1 angle in °		_____________________________

Leg 2 in mm		_____________________________

Leg 2 angle in °		_____________________________

Diagonal cuts according to drawing no.___________________

Mitre cuts according to drawing no.	______________________

L-shape:							 _______________pcs.

Edge			rounded 	sharp

Length in mm		_____________________________

Back in mm 		_____________________________

Leg 1 in mm 		_____________________________

Leg 1 angle in ° 		_____________________________

Diagonal cuts according to drawing no ___________________

Mitre cuts according to drawing no_______________________

Round arc: 							_______________pcs.

Unwinding length x unwinding width: ____________________

Radius: ___________°

SERVICE

Cut rectangular according to measurements: 				_______________m²

Special cut (waterjet):				 			_______________rm

Mitre cut (45° for edges):							_______________rm

Small cuttings (< 0,7 m²):							_______________pcs.

Undercut anchor drilling for KEIL undercut anchor; hs=8.5			_______________pcs.

Though drilling: Diameter 8 mm for rivet attachment 				_______________pcs.

ACCESSORIES/FASTENING

Exposed fastening with rivet

Visible attachment with rivets for aluminium substructure.

Attachment with fixed and sliding points, fixed points must be produced with sleeves.

Attachments: Façade rivet of aluminium with head painting, head diameter 14/16mm, length depending on substructure and panel thickness.

Material: AIMg3 (material no. EN AW-5754 according to DIN EN 573-3:2003-10)

Rivet mandrel: non-corrosive steel (material no. 1.4541)

Fixed point sleeve of aluminium, outer diameter 7.7mm, length depending on panel thickness.

Material: AIMg3 (material no. EN AW-6060 according to DIN EN 573-3:2003-10)

Supplier:	Rieder Facades GmbH

Glemmerstraße 21, 5751 Maishofen, Österreich

T +43 6542 690844, office@rieder.cc, www.rieder.cc

Concealed fastening with undercut anchor

Concealed attachment with undercut anchor from Keil with setting depth 8.5mm. Screw length depending on substructure.

Approval number: ETA-06/0220

Supplier:	KEIL Befestigungstechnik GmbH
			PO box 1158, 51751 Engelskirchen, Germany

T +49 2263 807 0

mail@keil.eu, www.keil.eu

Concealed fastening by bonding with Sika Tack panel system

Concealed attachment by bonding with the SikaTack panel system from Sika on uncoated aluminium.

Approval number: Z-10.8-408 (supplementary notice on the general building-supervisory approval)

Supplier:	www.sika.com

CONTACT

Sales: 		Rieder Facades GmbH

Glemmerstraße 21

5751 Maishofen

Austria

T +43 6542 690 844

office@rieder.cc

www.rieder.cc

Production:	Rieder Faserbeton-Elemente GmbH

Bergstraße 3a

83059 Kolbermoor

Germany

T +49 8031 90167 0

office@rieder.cc

www.rieder.cc