Tender specification öko skin

Glassfibre reinforced concrete slats "öko skin" for facade cladding

Status: April 2024

General

Information in the text of the invitation for tender must be reviewed and, if necessary, supplemented for the object.

Further liability by Rieder Facades GmbH is excluded. This also applies to printing and writing mistakes and to any subsequent changes. The respective national laws, standards and preliminary remarks for advanced rear-ventilated façades amended from time to time shall apply.

Loading, storage and handling provisions of the manufacturer must be observed.

General construction technique permit

Glassfibre reinforced concrete panels "fibreC" to cover exterior walls are certified with a general construction technique permit (allgemeine Bauartgenehmigung) “Z-31.4-166".

Certificate of conformance Austria

Austrian Certificate of Conformance No.: Z-6.1.2-04-4772

öko skin concrete facade								__________________ m²

öko skin glassfibre reinforced concrete panels for covering outer walls, delivery and installation.

- öko skin glassfibre reinforced concrete panels, produced of mineral raw materials

- Size BASIC: 1800 x 147 x 13 mm

- Size PLUS: Width 70 - 302 mm, Length 700 - 2500 mm (Ratio Width to Length 1:10)

- Texture: standard

- Reinforcement by AR (alkaline-resistant) glassfibre reinforced as glass-fibre-reinforced strands and short fibres in the matrix

- Production method by extrusion

- Weight approx. 26-31.5kg/m²; depending on shade

- Area 0.2646 m², thickness 13 mm

- Bending tension resilience at least 18 N/mm² (MOR)**

- Elasticity modulus approx. 10,000N/mm²

- Frost resistance pursuant to EN 12467

- Building material class A1 not flammable pursuant to DIN 4102 | EN 13501

- Water impermeability pursuant to EN 12467

- Wet-dry test pursuant to EN 12467

- Crystalline silica < 0% - not detectable

- Surface protection: The surface is applied with a transparent hydrophobic coating by default.

**    MOR: Modus of Rupture; design values deviate from MOR according to national provisions. The national approvals and provisions on calculation of the rated resistance shall apply

Pallet delivery (öko skin BASIC): 144 slats = 38,1 m²

Loading, storage and handling provisions of the manufacturer must be observed.

Ventilated façade covers on existing substructure according to technical provisions and applicable standards.

Supplier öko skin:	Rieder Facades GmbH

Glemmerstraße 21, 5751 Maishofen, Österreich

T +43 6542 690 844, office@rieder.cc, www.rieder.cc

COLOURS

Colour collection greyscale:

polar white 				_____________m²

off-white 				_____________m²

ivory 				_____________m²

silvergrey 				_____________m²

chrome 				_____________m²

anthracite 				_____________m²

liquid black 				_____________m²

Colour collection bricky:

coralline				_____________m²

terracotta 				_____________m²

oxide red				_____________m²

burgundy				_____________m²

merlot				_____________m²

Colour collection timber:

larch				_____________m²

oak					_____________m²

walnut				_____________m²

ebony				_____________m²

terra				_____________m²

Colour collection pietra:

cotton				_____________m²

vanilla				_____________m²

sahara				_____________m²

sandstone				_____________m²

almond				_____________m²

Other colours:

green				_____________m²

Surfaces

ferro: sandblasted surface			_____________m²

ferro light: slightly sandblasted surface	_____________m²

matt: smooth, matted surface		_____________m²

SPECIAL TEXTURE

vintage matt				_____________m²

SERVICE

Through drillings (per slat)			_______________pcs.

Grid drilling for öko skin hidden fix (per slat)	_______________pcs.

ÖKO SKIN STRIPES

öko skin in 3 different widths (70 mm, 147 mm and 302 mm), sequencing of slats is pre-defined

Length: 2500 mm, 3100 mm

Colour: 1 colour from colour collection greyscale

öko skin stripes easy: 1 colour in 2 surfaces ferro & ferro light		_______________m²

öko skin stripes bicolour: 2 colour in 3 surfaces ferro, ferro light & matt	_______________m²

ACCESSORIES/FASTENING

Visible fastening with rivet

Two attachment points must be provided as fixed points with a sleeve for attachment by rivet on an aluminium substructure.

Attachments:

Façade rivet of aluminium with head painting, head diameter 14/16mm, length depending on substructure and panel thickness. Material: AIMg3 (material no. EN AW-5754 according to DIN EN 573-3:2003-10)

Rivet mandrel: non-corrosive steel (material no. 1.4541)

Fixed point sleeve of aluminium, outer diameter 7.7mm, length depending on panel thickness. Material: AIMg3 (material no. EN AW-6060 according to DIN EN 573-3:2003-10)

Supplier rivets:		Rieder Facades GmbH

Glemmerstraße 21, 5751 Maishofen, Österreich

T +43 6542 690 844, office@rieder.cc, www.rieder.cc

Visible fastening with screw

When connecting by screw to a wood structure, every öko skin batten must be installed with at least 4 attachment points depending on installation pattern. Distance from the LE at most 600 mm, varying depending on installation pattern.

Façade screw A4, OSR T20 for wood substructures, head diameter 12 mm 5,5/45 mm, colour of screw head adjusted to öko skin colours.

Bores must be made on site.

Supplier screws:		Rieder Facades GmbH

Glemmerstraße 21, 5751 Maishofen, Österreich

T +43 6542 690 844, office@rieder.cc, www.rieder.cc

Concealed fastening with öko skin hidden fix

Rieder offers a calculation tool to determine the number of components. Please follow the installation instruction.

Standard back clip, L = 110 mm, aluminium black anodized (cut edge uncoated) (100 pcs/pkg.)	 __________pkg.

Self-drilling screw for clip, A2 black head - steel/aluminium inkl. bit (100 pcs/pkg.)		__________pkg.

Self-drilling screw for clip, A2 uncoated head - steel/aluminium inkl. bit (100 pcs/pkg.)		__________pkg.

Self-drilling screw for clip, A2 black head - timber inkl. bit (100 pcs/pkg.)			__________pkg.

Self-drilling screw for clip, A2 uncoated head - timber inkl. Bit (100 pcs/pkg.)			__________pkg.

RPA Rieder Power Anchor incl. Rubber washer (500 pcs/pkg.)				__________pkg.

Corner connector sheet, black anodized (cut edge uncoated (25 pcs/pkg.)			__________pkg.

Starter profile to bottom edge of facade, L = 1,8 m, aluminium black anodized

(cut edge uncoated) (10 pcs/pkg.)								__________pkg.

Starter profile to bottom edge of facade, L = 1,8 m, raw aluminium (10 pcs./pkg.)		__________pkg.

Top clip to top edge of facade, L=110 mm, aluminium black anodized (cut edge uncoated) (25 pcs./pkg.) _____pkg.

RPA Rieder Power Anchor drill bit set (driller + deep control stop)				__________pcs.

RPA Rieder Power Anchor drill bit								__________pcs.

Depth control stop for RPA Rieder Power Anchor drill bit					__________pcs.

Supplier öko skin hidden fix components:	Rieder Facades GmbH

Glemmerstraße 21, 5751 Maishofen, Österreich

T +43 6542 690 844, office@rieder.cc, www.rieder.cc

ADDITIONAL ITEMS

Substructure for rear ventilation level/assembly substrate öko skin 			__________________ m²

Delivery and installation of suitable substructure as assembly substrate for "öko skin glassfibre reinforced concrete slats", made of wood or aluminium (see below) acc. to structural requirements (structural engineering acc. to contractor)

Distance and arrangement of the carrying battens depending on installation pattern (300 – 600 mm) acc. to client's plan or structural engineering.

Attention: Specific installation patterns required a higher effort for the substructure.

Wood structure:

The wood structure must be made purs. to EN 338 using sufficiently dried wood (15% +/- 3%) with a cross-section of at least 100 x 30 mm.

Use of planed wooden battens is of benefit.

The battens must comply with the directives for construction timber pursuant to EN 338.

Joint tape: see dedicated item.

Aluminium structure:

Adjustable aluminium substructure according to plant annex and description.

Supplier:               ………………………………

The substructure must be flight-appropriate and perpendicular.

Substructure execution at window and door connections, inner and outer corners, sockets and roof edge connections as well as any attachments must be included in the unit price.

Scaffolding shall be settled separately.

Assembly öko skin 									__________________ m²

Delivery (FCA factory Kolbermoor, to the construction site without unloading) and installation

Assembly and handling installations of the manufacturer must be observed.

Incl. drilling of the öko skin depending on installation template

Incl. attachment media acc. to client (see technical description).

Cutting of fitted battens and all corner and edge formations must be included in the calculation.

Incl. all surcharges for execution of window and door connections, inner and outer corners, sockets and roof edge connections as well as any attachments.

Scaffolding shall be settled separately.

Ventilation grille										__________________ rm

Delivery and assembly of ventilation grilles pursuant to DIN 18516.

Material chosen by the client __________________

Mesh width: ___________________

Width: _______________________

Joint tape										__________________ rm

For wood substructures, joint tape must be installed as a weather protection.

Supply and install joint tape of plastic, rubber or neoprene

Width 110 mm or 70 mm (adjusted to LE, protrusion)

Façade sealing lane, wind paper								__________________ m²

Delivery and installation of the façade/sealing lane as a moisture barrier according to the manufacturer's processing directives.

Diffusion-open, UV- and weather-resistant

Material: e.g. DuPontTM Tyvek Uk Façade or equivalent

Offered system: _______________________

CONTACT

Sales: 		Rieder Facades GmbH

Glemmerstraße 21

5751 Maishofen

Austria

T +43 (0)6542 690 844

office@rieder.cc

www.rieder.cc

Production:	Rieder Faserbeton-Elemente GmbH

Bergstraße 3a

83059 Kolbermoor

Germany

T +49 (0)8031 90167 0

office@rieder.cc

www.rieder.cc